## Constant Flow Valves

1.0 Scope:

All requirements are for PVC Constant Flow Valves.

2.0 Materials:

U-PVC – Conforming to ASTM D1784 Cell Classification 12454 A

EPDM – Ethylene Propylene Diene Terpolymer Rubber

FKM – Viton® Fluorocarbon Rubber

ECTFE ( Ethylene/Chlorotrifluoroethylene

3.0 Valves:

All Constant Flow Valves shall be of solid thermoplastic flanged body construction.  1/2" – 3/4" shall be inline design while 1” – 4” shall be Y type design.  All Constant Flow valves shall have a calibrated flow dial and position indicator.  Valve accuracy shall be +/- 6% of full scale.  Internal valve spring shall be 304 SS with ECTFE coating.

3.1 Operators

Handwheel operator Asahi Standard valve handle Red color.

3.2 Approved Manufacturer

Valves shall be provided by Asahi/America, Inc. of Lawrence, MA with no approved equals.  Manufacturer must be ISO-9001 certified.

3.3 Pressure Vs. Temperature

Valves shall have a pressure rating of:   150 psi at 700 F all sizes

4.0 Accessories:

# 4.1 Actuation

There is no actuation available for the Constant Flow Valves.

5.0 Installation Procedures:

All valve joints shall be flanged and shall be prepared according to the instructions detailed in the Constant Flow Valve O & M manual.  All accessories should be installed in accordance with the manufacturer’s requirements as well as any facility requirements.