## Plasgear™ Gear-Operator

1.0 Scope:

All requirements are for valves requiring Gear-Operators for general usage, corrosive environments and freshwater submersible applications.

2.0 Materials:

Enclosure housing – Composite Plastic

Position Indicator - Polypropylene

Handwheel – Polypropylene Glass Filled

Output Coupling and Handwheel Bush – SCS13 (Cast SS)

Fasteners – 300 SS

Shaft -  300 SS

O-rings – Nitrile (Buna-n)

Worm & shaft gears – Beric

3.0 Plasgear™ Operators:

The Plasgear™ is the industry’s first all plastic enclosure gear-operator.  It is designed for highly corrosive environments and fresh water submersible applications.  The housing is sealed to the equivalent of Nema 6 submersible rating with IP67 corrosion resistance.  The Plasgear™ is designed for use on ¼ turn butterfly valves requiring up to a maximum output torque of 8,000 inch-pounds.

4.0 Models:

2 models are available:

Type-241 Plasgear™ - Maximum Output Torque – 2700 inch-pounds

ISO 5211 Bolt Circle – F07/F10

Gear Ratio – 38 : 1

Turns to Close – 9.5

Maximium Handwheel Force – 70 Foot-pounds

Weight – 5 lbs.

Type-243 Plasgear™ – Maximum Output Torque – 8,000 inch-pounds

ISO 5211 Bolt Circle – F14

Gear Ratio – 38 : 1

Turns to Close – 9.5

Maximum Handwheel Force – 90 foot-pounds

Weight – 18 lbs.

4.1 Approved Manufacturer

Plasgear™ Gear-Operators shall be provided by Asahi/America, Inc. of Lawrence, MA with no approved equals.  Manufacturer must be ISO-9001 certified.

4.2 Working Temperature:

-5°F  to  250°F

5.0 Installation Procedures:

The Plasgear™ would either come factory equipped on Asahi Type-57/57IL/57LIS or 56 Butterfly valves, or can be fitted to any manufacturer’s butterfly valves utilizing either a mounting bracket assembly or direct ISO mount.